MINI PROJECT

IMPACT OF RICE HUSK ASH ON CEMENT CONCRETE

(LAB REPORT)

RICE HUSK ASH (RHA) PROPERTIES:

- SPECIFIC GRAVITY:

WEIGHT OF EMPTY PYCNOMETER (M1)			: 324.5g

WEIGHT OF PYCNOMETER + RICE HUSK ASH (M2)		: 355.9g

WEIGHT OF PYCNOMETER + RHA + WATER (M3)		: 856.3g

WEIGHT OF PYCNOMETER +WATER (M4)			: 871.7g

SPECIFIC GRAVITY OF RHA : M2-M1 / (M2-M1)-(M4-M3)

= 1.96

SPECIFIC GRAVITY OF RHA = 1.96

- BULK DENSITY :

EMPTY WEIGHT OF CALIBRATED CONTAINER 	: 47g

WEIGHT OF CONTAINER + RHA 				: 96.6g

VOLUME OF CONTAINER  				:100 cm3

BULK DENSITY OF RHA 	= (96.6-47) / 100

= .496 g/cm3

= 496 kg/m3

BULK DENSITY OF RHA : .496 g/cm3 i.e 496 kg/m3

- FINENESS OF RHA:

MASS OF SAMPLE OF RHA		: 100g

MASS PASSING 90 MICRON SIEVE 	: 40g

FINENESS OF RHA  = 60%

High value due to ineffective grinding of sample.

EFFECT ON CEMENT AND CONCRETE:

- WORKABILITY:

- SLUMP TEST

0-25mm SLUMP LOW WORKABILITY

25-75mm SLUMP MEDUIM WORKABILITY

75-100mm SLUMP HIGH WORKABILITY

- FOR 43 GRADE SANKAR OPC,0% RHA :

| WATER CONTENT % | SLUMP (mm) |
| --- | --- |
| 0.45 | 0 |
| 0.55 | 42 |
| 0.60 | 95 |

HIGH WORKABLILITY AT 0.60 WATER CONTENT

- FOR SAME WATER CONTENT,AT DIFFERENT REPLACEMENT %

| % REPLACEMENT | WATER CONTENT % | SLUMP (mm) |
| --- | --- | --- |
| 0 | 0.50 | 13 |
| 10 | 0.50 | 5 |
| 20 | 0.50 | 3 |
| 30 | 0.50 | 0 |
| 40 | 0.50 | 0 |

WORABILITY OF THE MIX REDUCES GREATLY AS THE PERCENTAGE REPLACEMENT OF RHA INCREASES.

- VARYING WATER CONTENT ACCORDING TO STUDY PROVIDED ON LITERATURE

| % REPLACEMENT | WATER CONTENT | SLUMP (mm) |
| --- | --- | --- |
| 0 | 0.50 | 13 |
| 10 | 0.54 | 10 |
| 20 | 0.55 | 7 |
| 30 | 0.56 | 0 |
| 40 | 0.57 | 0 |

VARYING THE WATER CONTENT SLIGHTY ACCORDING TO DATA GIVEN IN STUDY DOES NOT GIVE WORKABLE MIX.

- TO FIND HIGH WORKABILITY WATER CONTENT FOT DIFFERENT PERCENTAGE (%) REPLACEMENTS.

- 10 % REPLACEMENT

| WATER CONTENT | SLUMP (mm) |
| --- | --- |
| 0.54 | 10 |
| 0.50 | 25 |
| 0.65 | 40 |
| 0.70 | 100 |

0.70 WATER CONTENT REQURED FOR HIGH WORKABLE MIX.

- 20 % REPLACEMENT

| WATER CONTENT | SLUMP (mm) |
| --- | --- |
| 0.55 | 7 |
| 0.60 | 13 |
| 0.65 | 25 |
| 0.70 | 42 |
| 0.75 | 60 |
| 0.80 | 86 |

0.80 WATER CONTENT REQUIRED FOR HIGH WORABLE MIX.

- 30 % REPLACEMENT

| WATER CONTENT | SLUMP |
| --- | --- |
| 0.56 | 0 |
| 0.60 | 6 |
| 0.65 | 14 |
| 0.70 | 21 |
| 0.75 | 40 |
| 0.80 | 59 |
| 0.85 | 82 |

0.85 WATER CONTENT REQUIRED FOR HIGH WORKABILITY MIX.

- 35 % REPLACEMENT

ACCORDING TO STUDY PROVIDED IN DATA MAXIMUM STRENGTH IS ACHIEVED AT 35 % REPLACEMENT OF RHA.

| WATER CONTENT | SLUMP (mm) |
| --- | --- |
| 0.60 | 5 |
| 0.65 | 13 |
| 0.70 | 17 |
| 0.75 | 30 |
| 0.80 | 55 |
| 0.90 | 80 |

0.90 WATER CONTENT IS REQUIRED TO GET A HIGH WORAKABLE MIX THAT PROVIDES MAXIMUM STRENGTH.

A HIGHLY WORABLE MIX AT 40% REPLACEMENT TEST NOT CARRIED OUT AS IT WOULD NOT BE TO GET DUE TO HIGH WATER CONTENT OF PRECEDING REPLACEMENTS.

- NORMAL CONSISTENCY.

- FOR 43 GRADE OPC .

| WATER CONTENT | INITIAL READING | FINAL READING | HT. NOT PENETRATED.(mm) |
| --- | --- | --- | --- |
| 0.30 | 0 | 9 | 9 |
| 0.31 | 0 | 6 | 6 |

NORMAL CONSISTENCY OF 43 GRADE OPC CEMENT=31%

- 10% REPLACEMENT

| WATER CONTENT | INITIAL READING | FINAL READING | HT.NOT PENETRATED (mm) |
| --- | --- | --- | --- |
| 0.31 | 0 | 40 | 40 |
| 0.40 | 0 | 25 | 25 |
| 0.45 | 0 | 0 | 0 |
| 0.42 | 0 | 11 | 11 |
| 0.43 | 0 | 5 | 5 |

NORMAL CONSISTENCY OF 90% OPC, 10% RHA = 43%

- 20 % REPLACEMENT

| WATER CONTENT | INITIAL READING | FINAL READING | HT. NOT PENETRATED (mm) |
| --- | --- | --- | --- |
| 0.43 | 0 | 38 | 38 |
| 0.45 | 0 | 37 | 37 |
| 0.47 | 0 | 35 | 35 |
| 0.49 | 0 | 28 | 28 |
| 0.52 | 0 | 22 | 22 |
| 0.54 | 0 | 18 | 18 |
| 0.55 | 0 | 15 | 15 |
| 0.56 | 0 | 12 | 12 |
| 0.57 | 0 | 10 | 10 |
| 0.58 | 0 | 9 | 9 |
| 0.59 | 0 | 7 | 7 |

NORMAL CONSISTENCY OF 80%OPC, 20%RHA  = 59%

- 30 % REPLACEMENT.

| WATER CONTENT | INITIAL READING | FINAL READING | HT. NOT PENETRATED (mm) |
| --- | --- | --- | --- |
| 0.57 | 0 | 38 | 38 |
| 0.59 | 0 | 35 | 35 |
| 0.61 | 0 | 33 | 33 |
| 0.65 | 0 | 25 | 25 |
| 0.67 | 0 | 20 | 20 |
| 0.69 | 0 | 18 | 18 |
| 0.71 | 0 | 16 | 16 |
| 0.73 | 0 | 13 | 13 |
| 0.75 | 0 | 11 | 11 |
| 0.77 | 0 | 8 | 8 |
| 0.79 | 0 | 6 | 6 |

NORMAL CONSISTENCY OF 70% OPC, 30 % RHA = 79%

- INITIAL & FINAL SETTING TIME

- FOR 43 GRADE OPC.

| TIME (MINS) | DEPTH NOT PENETRATED (mm) |
| --- | --- |
| 5 | 0 |
| 10 | 0 |
| 15 | 0 |
| 20 | 0 |
| 25 | 0.5 |
| 30 | 0.5 |
| 35 | 0.5 |
| 40 | 0.5 |
| 45 | 1 |
| 50 | 1 |
| 55 | 1 |
| 60 | 1 |
| 65 | 2 |
| 70 | 5 |

INITIAL SETTING TIME         	: 70 MINS

FINAL SETTING TIME 		: 135 MINS

- 10 % REPLACEMENT.

| TIME (MINS) | DEPTH NOT PENETRATED (mm) |
| --- | --- |
| 5 | 0 |
| 10 | 0 |
| 20 | 0 |
| 30 | 0 |
| 40 | .5 |
| 50 | 1 |
| 60 | 1 |
| 80 | 2 |
| 100 | 3.5 |
| 110 | 4 |
| 120 | 5 |

INITIAL SETTING TIME : 120 MINS

FINAL SETTING TIME   : 300 MINS

- 20 % REPLACEMENT.

| TIME (MINS) | DEPTH NOT PENETRATED (mm) |
| --- | --- |
| 10 | 0 |
| 20 | 0 |
| 30 | 0 |
| 40 | 0 |
| 50 | 0 |
| 60 | .5 |
| 80 | .5 |
| 100 | 1 |
| 120 | 2.5 |
| 140 | 3 |
| 160 | 4 |
| 170 | 4.5 |
| 180 | 5 |

INITIAL SETTING TIME : 180 MINS

FINAL SETTING TIME    : 480 MINS

- 30 % REPLACEMENT

| TIME (MINS) | DEPTH NOT PENETRATED (mm) |
| --- | --- |
| 10 | 0 |
| 20 | 0 |
| 30 | 0 |
| 40 | 0 |
| 60 | 0 |
| 80 | .5 |
| 100 | 1 |
| 120 | 1 |
| 140 | 1.5 |
| 160 | 2 |
| 180 | 3 |
| 200 | 3 |
| 220 | 3.5 |
| 230 | 4 |
| 240 | 4.5 |
| 250 | 5 |

INITIAL SETTING TIME : 250 MINS

FINAL SETTING TIME    : >8 HOURS